29 Fabrics

corresponding to DR-CAFTA Commercial Availability Request:

23.2007.06.18.Fabric.Government of the Dominican Republic

|  | 2007 HTSUS Number | Quantity Requested (linear Meters) | Fabric Description |
| --- | --- | --- | --- |
| 1 | 5208.33 | 45,721 | 100% cotton woven fabric; warp yarn size: 102/2 metric; filling yarn size: 68/1 metric; 52 warp ends/cm; 43 filling picks/cm; 170 gm/sq.meter; 147 cm width; weave type:3 thread or 4 thread twill; (piece) dyed. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 2 | 5801.22.90 | 100,585 | 100% cotton woven fabric; warp yarn size: 27/1 metric; filling yarn size: 27/1 metric; 28 warp ends / cm.; 50 filling picks/cm; 298 gm/sq.meter; 142 cm. width; weave type: 5.5 wale/ cm. corduroy; (piece) dyed. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 3 | 5801.22.90 | 82,297 | 100% cotton woven fabric; warp yarn size: 20/1 metric; filling yarn size: 20/1metric; 25 warp ends/cm.; 50 filling picks/cm.; 305 gm./sq.meter; 142 cm width: weave type: 4.3 wales/cm. corduroy; (piece) dyed. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 4 | 5801.22.90 | 73,153 | 100% cotton woven fabric; warp yarn size: 20/1 metric; filling yarn size: 20/1 metric; 19 warp ends/cm.; 58 filling picks/cm; 403 gm./sq.meter; 142 cm width; weave type:3.1 wales/cm. corduroy; (piece) dyed; Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 5 | 5212.23.6060 | 23,775 | 55% cotton 45% linen woven fabric; warp yarn size: 18.6 metric; filling yarn size: 18.6/1metric; 237 gm./sq.meter; 145 cm. width; weave type: three thread or four thread twill; (piece) dyed. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 6 | 5212.23.6060 | 22,860 | 55% cotton 45% linen woven fabric; warp yarn size: 20/1 metric; filling yarn size 18.5/1 metric; 28 warp ends/cm.; 19 filling picks/cm.; 274 gm./sq. meter; 142 cm. width; weave type:three thread or four thread twill; (piece) dyed. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 7 | 5209.43.0050 | 114,301 | 100% cotton woven fabric; warp yarn size:102/2 metric; filling yarn size 102/2 metric;75 warp ends/cm.; 36 filling picks/cm.;224 gm./sq. meter; 142 cm. width; weave type: three thread or four thread twill; of yarns of different colors; check/plaid/stripe. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 8 | 5208.43 | 114,301 | 100% cotton woven fabric; warp yarn size: 102/2 metric; filling yarn size: 102/2 metric; 63 warp ends/cm.; 30 filling picks/cm.; 183 gm./sq. meter; 142 cm. width; weave type: three thread or four thread twill; of yarns of different colors; check/plaid/stripe. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 9 | 5212.23.6040 | 59,437 | 54% cotton 44% linen 2% spandex woven fabric; warp yarn size: 34/1 metric cotton/linen; filling yarn size: 22/1metric cotton/linen+126 metric spandex; 44 warp ends/cm.; 30 filling picks/cm; 271 gm./sq.meter; 132 cm. width; weave type: duck; (piece) dyed. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 10 | 5209.39.0020 | 169,166 | 98% cotton 2% spandex woven fabric; warp yarn size 76/1 metric cotton; filling yarn size: 27/1 metric cotton + spandex; 82 warp ends/cm.; 31 filling picks/cm.; 254 gm./ sq. meter; 137 cm. width; weave type: sateen; (piece) dyed. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 11 | 5209.39.0020 | 169,166 | 98% cotton 2% spandex woven fabric; warp yarn size: 54/1 metric cotton; filling yarn size: 54/1metric cotton + 225 metric spandex; 75 warp ends/cm; 31 filling picks/cm.; 230 gm./sq meter; 122 to 127 cm width; weave type: sateen; (piece) dyed. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 12 | 5209.32 | 182,882 | 97% cotton 3% spandex woven fabric; warp yarn size: 67/1metric cotton; filling yarn size: 27/1 metric cotton+126 metric spandex; 78 warp ends/cm; 25 filling picks/cm; 237 gm./sq.meter; 132 to 137cm. width; weave type: three thread or four thread twill; (piece) dyed. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 13 | 5209.39.0090 | 123,446 | 98% cotton 2% spandex woven fabric; warp yarn size 54/1metric cotton; filling yarn size: 54/1 metric cotton+225 metric spandex. 71 warp ends/cm; 31 filling picks/cm.; 230 gm/sq.meter; 122 to 127 cm. width; weave type: dobby; (piece) dyed. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 14 | 5208.32.4020 | 45,721 | 100% cotton woven fabric; warp yarn size: 67/1 metric; filling yarn size: 67/1 metric; 52 warp ends/cm; 39 filling picks/cm; 155 gm./sq. meter; 144 cm width; weave type: plain; (piece) dyed. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 15 | 5208.39.2090 | 59,437 | 100% cotton woven fabric; warp yarn size: 54/1 metric; filling yarn size: 67/1 metric; 159 gm./sq.meter; 142 cm. width: weave type: herringbone twill; (piece) dyed. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 16 | 5209.39.0080 | 77,725 | 100% cotton woven fabric; warp yarn size: 54/1 metric; filling yarn size: 54/1 metric; 67 warp ends/cm; 54 filling picks/cm.; 254 gm.sq. meter; 144 cm width; weave type: dobby; (piece) dyed. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 17 | 5211.31.0020 | 91,441 | 75% cotton, 25% nylon woven fabric; warp yarn size: 35.5/1 metric; filling yarn size: 35.5/1 metric slubyarn cotton+ 45 metric filament nylon; 41 warp ends/cm.; 22 filling picks/cm; 223 gm/sq. meter; 147 cm width: weave type: plain; (piece) dyed. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 18 | 5209.49.0090 | 45,721 | 100% cotton woven fabric; warp yarn size: 54/2 metric; filling yarn size: 33/1 metric; 31 warp ends/cm.; 24 filling picks/cm; 278 gm/sq meter; 142 to 145 cm width; weave type: 2x2 herringbone twill; of yarns of different colors. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 19 | 5515.11.00 | 800,110 | 64% polyester 33% rayon 3% spandex woven fabric; warp yarn size: 67/2 metric polyester/rayon; filling yarn size: 67/2 metric polyester/rayon+ 225 metric spandex; 39 warp ends/cm; 22 filling picks/cm.; 206 gm/sq. meter; 144 to146 cm. width; weave type: three thread or four thread twill; of yarns of different colors, check pattern. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 20 | 5515.11.00 | 800,110 | 64% polyester 33% rayon 3% spandex woven fabric; warp yarn size: 67/2 metric polyester/rayon; filling yarn size: 67/2 metric polyester/rayon + 225 metric spandex; 39 warp ends/cm; 22 filling picks/cm; 206 gm/sq. meter; 144 to 146 cm width; weave type: three thread or four thread twill; of yarns of different colors, plaid pattern; Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 21 | 5515.11.00 | 800,110 | 64% polyester 33% rayon 3% spandex woven fabric; warp yarn size: 67/2 metric polyester/rayon; filling yarn size: 67/2 metric + 225 metric spandex; 39 warp ends/cm; 22 filling picks/cm; 206 gm/sq. meter; 144 to 146 cm. width; weave type: plain; of yarns of different colors. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 22 | 5515.11.00 | 800,110 | 64% polyester 33% rayon 3% spandex woven fabric; warp yarn size: 67/2 metric polyester/rayon; filling yarn size: 67/2 metric polyester/rayon + 225 metric spandex; 39 warp ends/cm.; 22 filling picks/cm; 206 gm./sq. meter; 144 to 146 cm. width; weave type: three or four thread twill; of yarns of different colors. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 23 | 5515.11.00 | 800,110 | 64% polyester 33% rayon 3% spandex woven fabric; warp yarn size: 67/2 metric polyester/rayon; filling yarn size: 67/2 metric polyester/rayon + 225 metric spandex; 39 warp ends/cm; 22 filling picks/cm.; 206 gm/sq meter 144 to 146 cm. width; weave type: dobby; of yarns of different colors. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 24 | 5211.32.0020 | 1,143,014 | 55% cotton 45% lyocell woven fabric; warp yarn size: 67/2 metric; filling yarn size: 67/2 metric; 230 gm./sq. meter; 149 cm width; weave type: herringbone twill; (piece) dyed. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 25 | 5801.32 | 1,143,014 | 86% polyester 14% nylon woven fabric; warp yarn size: 60 metric filament polyester; filling yarn size: 60 metric filament polyester + 56 metric filament nylon; 28 warp ends/cm; 63 filling picks/cm.; 250 gm/sq. meter; 150 cm. width; weave type: 3 wales per cm. corduroy;( piece) dyed. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 26 | 5515.11.00.05 | 640,088 | 70% polyester 30% viscose rayon woven fabric; warp yarn size: 50/2 metric; filling yarn size: 50/2 metric; 24 warp ends/cm; 21 filling picks/cm; 254 gm./sq. meter; 152 cm width; weave type: four thread (2x2) twill; of yarns of different colors, plaid pattern. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 27 | 6005.34.0010 | 114,301 | 100% polyester napped open work warp knit fabric; 152 to 163 cm. width; 118 gm./sq. meter; printed; flame retardant for children's sleepwear. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 28 | 5209.41.6020 | 685,808 | 100% cotton woven fabric; warp yarn size: 33/2 metric; filling yarn size: 20/3 metric; 39 warp ends/cm; 8 filling picks/cm.; 220 gm/sq. meter; 157 cm width; weave type: poplin; of yarns of different colors. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |
| 29 | 5209.42.0020 | 685,808 | 100% cotton woven fabric; warp yarn size: 20/1 metric; filling yarn size: 20/1 metric; 11 warp ends/cm.; 7.8 filling picks/cm; 291 gm./sq. meter; 154 cm. width; three thread or four thread twill; of yarns of different colors. Variance allowance of up to three percent for yarn size, thread count, fabric weight, and fabric width. |